## Slide 1: Low carbon asphalt using bio-based binders
Donna James & Gordon Airey
November 2025

## Slide 2
  Net Zero Highways plan (2021)
  Net Zero Highways – zero carbon roadmap for asphalt (2022)
Focused on asphalt surface courses - 63% of all asphalt used on the SRN in 2020.
Where did we start?

## Slide 3
Objective: develop a pro-active strategy for adoption of suitable technologies as part of the Net Zero Asphalt Roadmap.
Forward-facing project - reviewing the National Highways standards, understanding barriers and developing roadmap to accelerate early adoption of emerging technologies.
Future Asphalt Surface Course linking to NH Net Zero

## Slide 4: Collaboration is key
Extensive collaboration to successfully deliver trials:
Trial design
Departure from Standard Approval
Mix Design
Binder supply
Programme
Installation
Sampling & testing

## Slide 5
Low Carbon Materials Testing
University of Nottingham - Nottingham Transportation Engineering Centre

## Slide 6
Phase 1 -
A30 Bio-based Binder Trial​
Two commercially available PMB bio-based binders installed within Thin Surface Course System
Hot mix with no reclaimed asphalt
Control also installed
First surface course with bio-based binder on the SRN in England
Approval via a Departure from Standard

## Slide 7
  Phase 2 focussed on combining de-carbonisation levers of bio-based binders with warm-mix asphalt & increased reclaimed asphalt to maximise carbon reduction
  A2 Kingston
      Bio-based PMB
      Bio-based PMB & Warm
      Bio-based PMB & Warm & 20% RA
  A34 East Ilsley
      Bio-based PMB
      Bio-based PMB & Warm
      Bio-based PMB & Warm & 20% RA
      Bio-based PMB & Warm & 30% RA
Phase 2 – Stacking Technologies

## Slide 8
A30 Trial Bio-based Binder Properties BS EN 14023 Classification
Property | Test Method | Binders Installed on the A30 |  | 
 |  | Control 1 | Bio-binder 1 | Bio-binder 2
Penetration @ 25oC | EN 1426 | 7 | 7 | 7
Softening Point | EN 1427 | 3 | 3 | 3
Force Ductility @ 5oC | EN 13589 / EN 13703 | 3 | 3 | 3
Change in mass | EN12607-1 | 3 | 2 | 3
Change in Softening Point | EN 1427 | 2 | 2 | 2
Retained Penetration | EN 1426 | 7 | 7 | 7
Elastic Recovery @ 25oC | EN 13398 | ND | 2 | ND
Flash Point | EN ISO 2592 | 2 | 2 | 2

## Slide 9
A30 - Gyratory Compaction
The compactability of the asphalt mixtures was assessed by gyratory compaction in accordance with BS EN 12697-10 and BS EN 12607-31

## Slide 10
A30 Wheeltracking - Small Device Procedure B @60oC
Wheeltrack testing was conducted in accordance with BS EN 12697-22 Procedure B in Air at 60oC.
The Small Device utilises a solid rubber tyre and applies a load of 700N.
All test results complied with the requirements for the PD 6691 Table B.4 “Very heavily stressed sites requiring very high rut resistance” with WTSAIR<0.8

## Slide 11
Wheeltracking testing was conducted in accordance with BS EN 12697-22 using the Large Device. Testing was undertaken for 30,000 passes at 60oC.
The Large Device uses a pneumatic tyre and applies a high load of 5,000N
All trial sections readily achieve the Pmax5 category in accordance with BS EN 13108-1.
A30 Wheeltracking - Large Device @60oC

## Slide 12
A30 Water Sensitivity – Indirect Tensile Strength Ratio (ITSR)
Moisture damage can be defined as the loss of strength of asphalt mixtures due to the presence of water
Resistance to moisture damage is evaluated by means of the water sensitivity test in accordance with BS EN 12697- 12 (Method A)
The required water sensitivity requirements for Thin Surface Course Systems on SRN in England are defined by SHW Clause #942
The water sensitivity of mixtures conforming with BS EN 13108 Parts 1, 2 and 5 shall conform to, at least, category ITSRmin70
Asphalt Mixture | Indirect Tensile Strength Ratio (%)
Control 1 | 96.0
Bio-binder Trial Section 1 | 100.0
Bio-binder Trial Section 2 | 95.0

## Slide 13
  A2 Kingston – First warm mix surface course with bio-based binder & reclaimed asphalt installed on the SRN

## Slide 14
Wheeltrack testing was conducted in accordance with BS EN 12697-22 Procedure B in Air at 60oC
All test results complied with the requirements for the PD 6691 Table B.4 “Very heavily stressed sites requiring very high rut resistance” with WTSAIR<0.8
Chart: Number of Load Cycles
Error Control + 0% RA (Warm) | 1.455 | 1.57 | 1.655 | 1.73
Error Bio + 0% RA (Hot) | 1.755 | 1.915 | 2.03 | 2.095
Error Bio + 0% RA (Warm) | 1.38 | 1.525 | 1.625 | 1.67
Error Bio + 20% RA (Warm) | 1.39 | 1.505 | 1.57 | 1.615
A2 Wheeltracking - Small Device Procedure B @60oC

## Slide 15
  Indirect Tensile Stiffness Modulus (20oC)
  Indirect Tensile Strength Ratio
Mix Ref | Bituminous Mixture | Mean Indirect Tensile Stiffness Modulus (MPa)
1 | Control + 0% RA (Warm) | 3500
2 | Bio + 0% RA (Hot) | 3100
3 | Bio + 0% RA (Warm) | 2600
4 | Bio + 20% RA (Warm) | 3900
Mix Ref | Bituminous Mixture | Indirect Tensile Strength Ratio (%)
1 | Control + 0% RA (Warm) | 100.0
2 | Bio + 0% RA (Hot) | 98.0
3 | Bio + 0% RA (Warm) | 102.0
4 | Bio + 20% RA (Warm) | 93.0
A2 Stiffness and Water Sensitivity

## Slide 16
  A2 Binder Rheology - Black Space Diagram (unaged)
Chart: Phase Angle (o)

## Slide 17
  A2 Recovered Binder Properties
Chart: Frequency (Hz)
Chart: Phase Angle (o)

## Slide 18
Carbon Calculations – Measurable Results
Using benchmark results for generic estimates (using actual mix designs and default values for other factors consistent with the Road Map).
A1-A5 emissions per tonne of asphalt (kgCO2e/t)
Chart: % Reduction in CO2e
| PMB 0% RA Warm | PMB 10% RA Warm | PMB 50% RA Warm | Bio PMB 0% RA Hot | Bio PMB 0% RA Warm | Bio PMB 20% RA Warm | Bio PMB 30% RA Warm
 | 0 | -3.1107 | -12.0311 | -14.1583 | -19.236 | -21.3632 | -22.5984