## Slide 1: EUROBITUME
THE EUROPEAN BITUMEN ASSOCIATION
Binder Innovations

## Slide 2: Innovation, Quality & Cost
“Innovation is seeing what everyone has seen & thinking what nobody has thought”
Dr. Albert Szent-György
“The bitterness of poor quality remains long after the sweetness of low price is forgotten”
Benjamin Franklin

## Slide 3: Innovations / Developments
Paving grade / pen bitumen
Hard paving / multigrades
Polymer-modified bitumen
Warm mix
Bio-based binders
Long life binders
Recycling binders
Foam mix
Cold mix
Combination of technologies
Binder innovations mirrored by asphalt innovations
Notes: First references for each system?

## Slide 4: Benefits of Innovation
Temperature susceptibility
  Polymer-modified bitumen
Flexibility
  Polymer-modified bitumen
Stiffness
  High modulus binders
Durability
  Long life
Application temperature
  Warm mix, cold mix
Effective use of raw materials
  Recycling, secondary materials,bio-based binders
Lower carbon materials
Longer life asphalt
Longer life asphalt
Reduced environmental impact
Reduced environmental impact
Reduced environmental impact
Notes: PIARC World Road Association review 2019
4 major categories: recycled asphalt, lower production temperatures, upgrading material at end of life
Increasing use of recycled / secondary materials, Increasing polymer use. Increasing biofuels . Increasing warm-mix
Biofuel reduction up to 60% CO2
Rolling resistance
Innovations are aligned in bitumen & asphalt

## Slide 5: Durability
Air, uv, moisture damage
Surface deformation & cracking
Increasing traffic
Increasing HGVs
Electric HGVs
Platooning
Climate change
Warmer & wetter?
Possibility of 5 maintenance interventions
Deterioration & failure
Notes: Possibility of maintenance every 10-12 years

## Slide 6: Durability
Longer life construction
Possible reduction to 3 maintenance interventions

## Slide 7: Longer-life binders
Reduced rate of oxidation
Reduced rate of hardening
Improved flexibility
A2, A34, A43

## Slide 8: Reducing Carbon Impact
Lower carbon binders
Biogenic components
  Plant-based materials
A30, A452, A92
Notes: Effect of calculation method / perspective etc

## Slide 9: Reducing Temperature
Stack gas emission reduction
Job-site emission reduction
Less binder ageing
Less thermal stress
A better working environment
Warm mix technology growing
Foam mix technology growing
Notes: Using warm mix is not just about the temperature
Now in SHW
Now in BS 594987
Figures how warm mix increase in Europe. Much greater adoption in USA

## Slide 10: Climate Change
2007
2010
2022
Notes: Climate is changing. But in what way? Less on global warming more on overall change.
More flooding – pavements under water for days / weeks (Ian Walsh anecdote)
Record low: -27C 1995
Record high: 40.3C 2022

## Slide 11: Temperature Susceptibility
Chart: Temperature/ °C
| 20/30 | 30/45 | 40/60 | 50/70 | 70/100 | 100/150 | 160/220 | 250/330 | PMB1 | PMB2
BP | -3 | -5 | -7 | -8 | -10 | -12 | -15 | -16
SP | 59 | 56 | 52 | 50 | 47 | 43 | 39 | 34
Glassy
Brittle
Fretting
Soft
Viscous
Rutting

## Slide 12: Temperature Susceptibility
Chart: Temperature/ °C
| 20/30 | 30/45 | 40/60 | 50/70 | 70/100 | 100/150 | 160/220 | 250/330 | PMB1 | PMB2
BP | -3 | -5 | -7 | -8 | -10 | -12 | -15 | -16 | -22 | -28
SP | 59 | 56 | 52 | 50 | 47 | 43 | 39 | 34 | 62 | 85
Glassy
Brittle
Fretting
Soft
Viscous
Rutting

## Slide 17
Notes: Picture of road failure on A140

## Slide 22
10mm SMA to PD6691 with PMB Binder
50/20 HRA binder course with PMB binder
Bituminous, Stress Absorbing Membrane Interlayer with a PMB binder
Continually Reinforced Concrete Pavement, 20mm Flint Gravel
Hydraulically Bound Material, 20mm gravel (Probably CBM 4)
Thermocouple
Thermocouple
Thermocouple
Thermocouple
Thermocouple
Notes: SO how do we know that we're not wasting our time with some of the things i've just mentioned
Changing Climates and temperatures are very relevant the pavement design
During the construction work at scole we placed thermocouples in the pavement as it was being built.
To see if road temperature affect the pavement, or if they will in the future
And to look at How far temperatures penetrate below the surface?

## Slide 26
Chart: Temperature Fluctuations throughout 17th May 2024
| 1.3888888888888888E-2 | 3.4722222222222224E-2 | 5.5555555555555552E-2 | 7.6388888888888895E-2 | 9.7222222222222224E-2 | 0.11805555555555557 | 0.1388888888888889 | 0.15972222222222224 | 0.18055555555555555 | 0.20138888888888887 | 0.22222222222222221 | 0.24305555555555555 | 0.2638888888888889 | 0.28472222222222221 | 0.30555555555555552 | 0.3263888888888889 | 0.34722222222222227 | 0.36805555555555558 | 0.3888888888888889 | 0.40972222222222227 | 0.43055555555555558 | 0.4513888888888889 | 0.47222222222222227 | 0.49305555555555558 | 0.51388888888888895 | 0.53472222222222221 | 0.55555555555555558 | 0.57638888888888895 | 0.59722222222222221 | 0.61805555555555558 | 0.63888888888888895 | 0.65972222222222221 | 0.68055555555555547 | 0.70138888888888884 | 0.72222222222222221 | 0.74305555555555547 | 0.76388888888888884 | 0.78472222222222221 | 0.80555555555555547 | 0.82638888888888884 | 0.84722222222222221 | 0.86805555555555547 | 0.88888888888888884 | 0.90972222222222221 | 0.93055555555555547 | 0.95138888888888884 | 0.97222222222222221 | 0.99305555555555547
400mm below RL | 18.22 | 18.16 | 18.11 | 18.1 | 18.09 | 18.05 | 17.96 | 17.93 | 17.81 | 17.76 | 17.7 | 17.67 | 17.49 | 17.36 | 17.32 | 17.11 | 16.76 | 16.36 | 16.58 | 16.41 | 16.62 | 16.63 | 16.87 | 16.76 | 16.72 | 16.97 | 17.34 | 17.57 | 17.67 | 17.87 | 18.07 | 18.33 | 18.5 | 18.68 | 18.9 | 19.03 | 19.2 | 19.37 | 19.48 | 19.57 | 19.59 | 19.61 | 19.65 | 19.71 | 19.74 | 19.75 | 19.74 | 19.73
300mm Below RL | 17.6 | 17.53 | 17.43 | 17.4 | 17.31 | 17.27 | 17.22 | 17.14 | 17.06 | 16.97 | 16.88 | 16.79 | 16.75 | 16.66 | 16.62 | 16.5 | 16.43 | 16.45 | 16.52 | 16.49 | 16.74 | 16.76 | 17.03 | 17.02 | 17.36 | 17.68 | 18.09 | 18.13 | 18.33 | 18.64 | 18.82 | 19.18 | 19.36 | 19.51 | 19.65 | 19.79 | 19.86 | 19.95 | 20.07 | 20.08 | 20.11 | 20.09 | 20.07 | 20.02 | 19.93 | 19.83 | 19.76 | 19.65
200mm Below RL | 17.18 | 17.03 | 16.95 | 16.83 | 16.72 | 16.66 | 16.6 | 16.54 | 16.38 | 16.25 | 16.1 | 15.97 | 15.88 | 15.81 | 15.8 | 15.79 | 15.9 | 16.14 | 16.47 | 16.7 | 17.15 | 17.55 | 18.01 | 18.36 | 18.86 | 19.49 | 20.17 | 20.53 | 20.68 | 20.98 | 21.26 | 21.56 | 21.78 | 21.85 | 21.84 | 21.82 | 21.75 | 21.69 | 21.66 | 21.52 | 21.41 | 21.23 | 21.04 | 20.81 | 20.55 | 20.27 | 20.03 | 19.74
175mm Below RL | 17 | 16.82 | 16.6 | 16.54 | 16.47 | 16.39 | 16.33 | 16.24 | 16.06 | 15.86 | 15.7 | 15.58 | 15.49 | 15.38 | 15.44 | 15.48 | 15.63 | 16.04 | 16.57 | 16.98 | 17.68 | 18.24 | 18.92 | 19.27 | 19.91 | 20.74 | 21.7 | 21.95 | 22 | 22.29 | 22.61 | 22.91 | 23.09 | 22.99 | 22.87 | 22.71 | 22.55 | 22.41 | 22.27 | 22.06 | 21.84 | 21.56 | 21.26 | 20.94 | 20.63 | 20.26 | 19.88 | 19.58
100mm below RL | 15.9 | 15.64 | 15.57 | 15.5 | 15.41 | 15.3 | 15.2 | 14.96 | 14.72 | 14.51 | 14.34 | 14.17 | 14.09 | 14.27 | 14.53 | 14.87 | 15.4 | 16.34 | 17.37 | 18.25 | 19.39 | 20.31 | 21.23 | 21.83 | 23.04 | 24.3 | 25.2 | 25.04 | 25.03 | 25.38 | 25.61 | 25.66 | 25.42 | 25.02 | 24.58 | 24.16 | 23.72 | 23.38 | 22.96 | 22.53 | 22.06 | 21.49 | 20.95 | 20.35 | 19.79 | 19.33 | 18.81 | 18.37
40mm below RL | 15.42 | 15.25 | 15.41 | 15.4 | 15.3 | 15.29 | 14.48 | 13.77 | 13.27 | 12.77 | 12.5 | 13.59 | 13.87 | 14.48 | 15.01 | 15.92 | 17.25 | 19 | 20.09 | 21.14 | 22.24 | 23.8 | 24.48 | 26.23 | 28.16 | 29.76 | 27.96 | 27.11 | 27.9 | 28.35 | 28.1 | 27.62 | 26.56 | 25.78 | 24.99 | 24.28 | 23.87 | 23.25 | 22.55 | 21.85 | 21.03 | 20.19 | 19.41 | 18.73 | 18.11 | 17.57 | 17.14 | 16.68
3mm below RL | 12.7 | 13.39 | 13.44 | 13 | 12.95 | 12.64 | 12.09 | 11.68 | 11.34 | 11.17 | 11.25 | 11.5 | 12.57 | 13.75 | 14.68 | 16.09 | 20.21 | 22.68 | 24.98 | 28.06 | 26.68 | 28.7 | 27.07 | 35.88 | 37.45 | 34.75 | 29.82 | 32.49 | 33.54 | 31.83 | 32.17 | 28.57 | 27.84 | 26.7 | 25.34 | 24.57 | 24.06 | 22.71 | 21.77 | 20.63 | 19.48 | 18.41 | 17.47 | 16.73 | 16.04 | 15.77 | 15.26 | 15.06
Air | 7.84 | 8.8 | 9.43 | 9.26 | 9.09 | 9.03 | 8.65 | 8.35 | 8.94 | 9.67 | 9.78 | 8.31 | 10.63 | 12.08 | 12.01 | 14.28 | 16.71 | 16.99 | 18.45 | 20.52 | 21.18 | 21.39 | 19.69 | 22.92 | 23.16 | 23.93 | 21.9 | 23.38 | 24.01 | 23.38 | 24.01 | 20.82 | 20.62 | 20.5 | 19.83 | 19.11 | 19.15 | 17.65 | 17.04 | 15.96 | 14.94 | 13.33 | 12 | 11.16 | 10.55 | 10.23 | 9.86 | 9.91

## Slide 27
A470 Dolwyddelan, Wales
Data Courtesy of the Welsh Government
Notes: 40mm WGSMA
60mm SMA 14
80-100 AC 20 (slate waste bin/base)

## Slide 28: Temperature Susceptibility
Chart: Temperature/ °C
| 20/30 | 30/45 | 40/60 | 50/70 | 70/100 | 100/150 | 160/220 | 250/330 | PMB1 | PMB2
BP | -3 | -5 | -7 | -8 | -10 | -12 | -15 | -16 | -22 | -28
SP | 59 | 56 | 52 | 50 | 47 | 43 | 39 | 34 | 62 | 85
Glassy
Brittle
Fretting
Soft
Viscous
Rutting